## Slide 1: The Development and Study of Organic Composites
Timothy Cotter (ME)
Allyson Kearns (CHE, minor ME)
Allison Sichler (CHE, minor SE)
Aiden Wright (ME)

## Slide 2: Introduction
In an effort to alleviate modern society’s reliance on petroleum-based plastics, our team explored compostable alternatives via organic fiber-reinforced composites.

## Slide 3: Objectives
To develop a novel composite material made from bioplastic resins, reinforced with natural fibers
To explore the properties of the composite including: matrix-fiber adhesion, degradability, material composition, and mechanical strength

## Slide 4: Characterization and Degradation
Material categorization
  Biodegradable
  Compostable
  Organic
Biodegradation
  Nutrient composition
  pH
  Gas exchange rates
  Temperature

## Slide 5: Fiber Reinforced Composites (FRC)
Chopped Fibers
Random Orientation

## Slide 6: Methodology
Add 2.5 g potato starch, 3 mL of HCl, and 2 mL of glycerol to 25 mL of water
Place the mixture on a hot plate at 200°C for 15 minutes, mixing every couple of minutes
Add 3 mL of NaOH and pour the mixture and chopped fibers into a mold
Allow it to set over night either at room temp, in an oven at 105°C, or in the presence of a vacuum

## Slide 7: Material Analysis
Jute, 100x
Cotton, 100x Jute, 100x Flax, 125x

## Slide 8: Material Analysis
Chart: Density Variation
| Potato Starch Polymer | Flexible Composite | High Flax Composite | Partial Vacuum Cure | Total Vacuum Cure
Series 1 | 2.88 | 2.7429 | 0.7871 | 2 | 3.5
Column1
Column2
Potato Starch Polymer
Flexible Composite
Total Vacuum Cure

## Slide 9: Material Analysis
Chart: Observed Degradation in Compost
| 0 | 8 | 12 | 29 | 43 | 55
Plain Potato | 3.6 | 2
Flexible Polymer | 4.8 | 2.1
High Flax Composite | 5.744 | 2.816 | 1.9 | 1.6 | 0.7
Partial Vacuum Cure | 2.6 | 1.8
Total Vacuum Cure | 3.5 | 2.8
Vinyl Ester | 10.6 | 10.6 | 10.6 | 10.6 | 10.6 | 10.6

## Slide 10: Material Analysis
Chart: Observed Degradation with Varying Conditions
| 0 | 8 | 18 | 29 | 36 | 41 | 54
Open Air | 4.8 | 4.8 | 4.9 | 4.8 | 4.8 | 4.9
Ocean Water | 5.612 | 2.796 | 2.5 | 2.5 | 2.5
Low Oxygen | 5.2 | 3.5
Column1
Column2
Column3
Notes: Swollen, opaque. Indicative of compostability not just biodegradability.

## Slide 11: Recommendations
Instron → Tensile Testing
Fourier-Transform Infrared Microscopy → Chemical Composition

## Slide 12: Recommendations
Thin-Flexible Plastic
Hard, High Strength Plastic
Create Samples in Vacuum
Corn-Starch Based Resins
Altered Fiber Orientation
Notes: vacuum, toy, thin flexible plastic, FTIR, Instron
orientation, new resin materials

## Slide 13
Questions?
Please feel free to contact us at
gr-mechem@wpi.edu
Or our advisors at
sjkmiotek@wpi.edu
guceri@wpi.edu